OXFORD - Technical Specifications

ISO 13006 - EN 14411 - ISO 10545 Standards

| Nominal sizes (cm): 6x25 |  | Thickness (mm): 9.5 |
| --- | --- | --- |
| Sides: Natural |  | Surface: Natural |
| Product Name: | Oxford Emerald, Oxford Taupe, Oxford Blue | Product Group: BIa- GL |

| Technical characteristics |  | Test method | EN 14411 and ISO 13006 requirements | Seramiksan Average values |
| --- | --- | --- | --- | --- |
| Dimensions | Length and width | ISO 10545-2 | ± %0.6 and ±2.0 mm | ± %0.6 and ±2.0 mm |
|  | Straightness of sides | ISO 10545-2 | ± %0.5 | ± %0.5 |
|  | Rectangularity | ISO 10545-2 | ± %0.5 | ± %0.5 |
|  | Flatness | ISO 10545-2 | ± %0.5 | ± %0.5 |
|  | Thickness | ISO 10545-2 | ± %5 | ± %5 |
| Water absorption |  | ISO 10545-3 | Max. %0.5 | Max. %0.5 |
| Modulus of rupture |  | ISO 10545-4 | 35 N/mm² | 35 N/mm² |
| Breaking strength (S) |  | ISO 10545-4 | > 1300 N | > 1300 N |
| Abrasion resistance |  | ISO 10545-7 | Declared value | PEI: 2 |
| Linear thermal expansion |  | ISO 10545-8 | Declared value | < 9.0x 10¯6 /C° |
| Thermal Shock Resistance |  | ISO 10545-9 | No alterations | Resistant |
| Frost resistance |  | ISO 10545-12 | No alterations | Resistant |
| Chemical resistance |  | ISO 10545-13 | Declared value | LA-HA |
| Household chemicals resistance |  | ISO 10545-13 | Min B. | A |
| Stain resistance |  | ISO 10545-14 | Min class 3 | Class 5 |
| Mohs Hardness |  | UNI EN 101 | Min.5 | 6 |
| Shade variation |  | ANSI A 137.1 | Not required | V4 |
| Fire reaction |  | UNI EN 13501-1 | - | A1FL class |